SECTION 10 17 16

TELEPHONE ENCLOSURES

PART 1 GENERAL

1.01   SUMMARY

- Equipment and materials used shall be standard components that are manufactured and available for purchase as standard replacement parts as long as the product is commercially available from the manufacturer.

1.02   QUALITY ASSURANCE

- All gooseneck pedestal mount installation, configurations, setup, program and related work shall be performed by electronic technicians thoroughly trained by the manufacturer in the installation and service of the equipment provided.

- The gooseneck pedestal mount shall be warrantied against any defects in material and workmanship under normal use for a period of five (5) years from date of installation, provided that manufacturer receives a completed "Installation Certification" certifying the date on which the system has been installed.  An "Installation Certification" card shall be enclosed with every unit.  In the event that no "Installation Certification" is received by manufacturer, the five (5) years will commence on the date of shipment by the manufacturer.

1.03   CERTIFICATIONS AND STANDARDS

- The gooseneck pedestal mount as an assembly shall be certified to:

UL Std 60950-1

PART 2 PRODUCTS

2.01   GENERAL

- The gooseneck pedestal mount shall:

  - Consist of a highly vandal-resistant free-standing steel emergency phone gooseneck pedestal mount.

2.02   HARDWARE

- The pedestal mount shall:

  - Be constructed of 1/8” thick, 2” O.D. square steel pipe and weigh approximately 20 lbs.

  - Measure 7.5” W x 12.5” D x 41.25” H.

  - Utilize a high-gloss, multi-coat, corrosion-inhibitive coating that shall be applied to withstand prolonged exposure to hard environments.

    - Gooseneck pedestal mount shall be sandblasted to SSPC-6 standards before a 2-3 mil layer of rust-inhibitive primer is applied.

    - Gooseneck pedestal mount shall be hand sanded for smoothness before a second 2-3 mil layer of primer is applied.

    - Gooseneck pedestal mount shall have a 2-3 mil layer of customer specified color coat applied.

    - Gooseneck pedestal mount shall have a 1-2 mil layer of clear coat applied.

- The gooseneck pedestal mount base plate shall:

  - Be constructed of 0.50” A-36 Structural Steel.

  - Have a 1.8” diameter center hole for wiring access.

  - Have four 0.50” holes for anchor bolt attachment.

  - Have an integrated base plate cover.

- The gooseneck pedestal mount shall have a mounting plate on the front to accommodate flush mounting an emergency phone surface mount at car height. The mounting plate shall:

  - Measure 10.5” H x 7.5” W.

  - Be centered 36” above the gooseneck pedestal base.

  - Have four 11/32” square holes to accommodate four 5/16” square neck bolts for surface mount attachment.

2.03   MANUFACTURED UNITS

- The gooseneck pedestal mount shall be a Talkaphone ETP-GP-C Emergency Telephone Gooseneck Pedestal Mount.

PART 3 EXECUTION

3.01      INSTALLATION

- The Contractor shall carefully follow instructions in documentation provided by the manufacturer to ensure all steps have been taken to provide a reliable, easy-to-operate system.

- All equipment shall be tested and configured in accordance with instructions provided by the manufacturer prior to installation.

END OF SECTION